Home < Material Details < PC Tolerances
PC Tolerances

Magnetic Tolerance Material (Mix No.) -2 -8 -14 -18 -19 -26 -28 -30 -33 -34 -35 -38 -40 -45 -52 -267 -275 AL Tolerance ±5% ±10% ±10% ±10% ±10% ±10% ±10% ±10% ±10% ±10% ±10% ±10% ±10% ±10% ±10% +35% -25% +35% -25% The cores are manufactured to the AL values listed; the permeability for each material is for reference only. In all cases, the AL values are based on a peak AC flux density of 10 guass (1mT) at a frequency of 10kHz. Measurements made under other conditions will produce results in accordance with the magnetic curves shown in the Percent Initial Permeability vs. Peak AC Flux Density Graph. The toroidal cores are tested with an evenly-spaced full single-layer winding in order to minimize leakage effects. Iron powder cores tested with a small number of turns which are not evenly distributed will produce higher inductance readings than expected. The E cores are tested with 100 turns. The Magnetic Characteristic curves shown are have a typical tolerance of ±10%. The curves on Core Loss characteristics have a typical tolerance of ±15%.

Dimensional Tolerances (inches) TOROIDS* OD ID Ht TOROIDS* OD ID Ht T16-T20 ±.010 ±.010 ±.010 T150-T225 ±.025 ±.025 ±.030 T25-T38 ±.015 ±.015 ±.020 T249-T400 ±.030 ±.030 ±.030 T40-T72** ±.020 ±.020 ±.020 T520-T650 ±.050 ±.050 ±.050 T44-T72** ±.020 ±.020 ±.020 T80-T141 ±.020 ±.020 ±.025 - COMPOSITE* OD ID Ht COMPOSITE* OD ID Ht ST50 ±.015 ±.015 ±.020 ST150 ±.040 ±.030 ±.030 ST83-ST102 ±.030 ±.020 ±.025 ST200 ±.050 ±.040 ±.040 - BUS BAR* A B D E L HS300-HS400 ±.015 ±.020 ±.005 ±.005 ±.020 - U CORES A B C E F G U61-U80 ±.010 ±.010 ±.010 ±.010 ±.010 ±.010 U350 ±.020 ±.020 ±.015 ±.020 ±.015 ±.030 - E CORES A B C D F G MAX GAP*** E49-E118 ±.010 ±.010 ±.005 ±.007 ±.005 ±.007 .0015 E125-E162 ±.015 ±.015 ±.007 ±.010 ±.007 ±.010 .0015 E168-E225 ±.015 ±.015 ±.010 ±.010 ±.007 ±.010 .0020 E305-E450 ±.030 ±.030 ±.015 ±.020 ±.015 ±.020 .0030 E610 ±.040 ±.040 ±.025 ±.030 ±.025 ±.030 .0050 - EF CORES A B C D E/F G MAX GAP*** EF60-EF80 ±.010 ±.010 ±.005 ±.010 ±.005 ±.007 .0030 - EM CORES A B C D G H MAX GAP*** EM145 ±.015 ±.015 ±.010 ±.020 ±.010 ±.015 .0020 EM168-EM220 ±.015 ±.015 ±.010 ±.020 ±.010 ±.015 .0030 - PLAIN CORES OD L Pxx24-Pxx40 +.000/-.005 ±.015 Pxx48-Pxx76 +.000/-.005 ±.020 - HOLLOW CORES OD ID L Hx10-Hx12 +.000/-.005 +.005/-.000 ±.010 Hxx14-Hxx20 +.000/-.005 +.005/-.000 ±.015 Hxx21-Hxx25 +.000/-.005 +.005/-.000 ±.020 - DISCS OD CB ID T D45-D80 +.000/-.010 +.005/-.000 +.005/-.000 ±.007 - *Tolerance includes coating **Gap per piece ** OD for T50-8/90 and T50-8B/90 is + 025/- .015

About Us | What We Do | Contact Us | Samples | Catalog | Thermal Aging | Parts | Materials | Software | Home